AlN Absorption Mechanisms

Literature review and alpha0 estimates for the loss-vs-dimensions absorption model

# Purpose

This document supports the non-uniform absorption model in the loss-vs-dimensions pipeline (absorption_model.py / plot_loss_vs_dimensions.py’s MECHANISMS list). Each mechanism there is parameterized by a LOCAL power-absorption coefficient at the interface/sidewall (alpha0, in dB/m) and a characteristic penetration depth (L, in nm) over which it decays into the core — the modal loss the pipeline actually reports is much smaller than alpha0, since it is the Poynting-flux-weighted average of this profile over the whole mode cross-section, not alpha0 itself. This review is an attempt to ground those alpha0 values in published measurements where possible, at or near the 450 nm pump wavelength used in the sweep.

Scope and method: sources were located via targeted literature search (see reference list) and, where full text was paywalled or unreadable, cross-checked against a second independent summary before being cited here. Nothing below should be read as a validated, device-specific measurement — see the caveats after the table.

# Summary table

| Mechanism | alpha0 estimate | Supporting assumptions | Reference |
| --- | --- | --- | --- |
| Dislocations (growth interface) | Not directly quantified in dB/m. Literature models this mechanism as SCATTERING, not absorption (see note). | Typical threading dislocation density in non-MOCVD AlN: 10⁸–10¹⁰ cm⁻². Volume-current-method analysis shows TM modes see measurably higher dislocation-induced loss than TE modes — relevant since the simulated mode here is TM00. | Chen et al., "Study of crystalline defect induced optical scattering loss inside photonic waveguides in UV–visible spectral wavelengths using volume current method," Opt. Express 27(12), 17262 (2019). |
| C impurities (growth interface) | ≈ 2.6–3.5×10⁴ dB/m (order-of-magnitude anchor; likely a high/conservative bound for photonic-grade thin films — see note). | Bulk PVT-grown AlN, [C] ≈ 7.5–10×10¹⁹ cm⁻³, [Si],[O] ≈ 2–9×10¹⁸ cm⁻³. Measured absorption coefficient 60–80 cm⁻¹ across a broad 2–4 eV (≈310–620 nm) band — not isolated to carbon alone. | Robinson et al., "Charge-state control of carbon-related optical absorption in AlN," arXiv:2606.19615 (2026). |
| O impurities (growth interface) | Same order-of-magnitude anchor as C (2.6–3.5×10⁴ dB/m, from the same co-doped samples) — wavelength relevance supported separately. | Yellow-coloration absorption band centered at 2.86 eV ≈ 434 nm — close to the 450 nm pump — attributed to aluminum-vacancy/oxygen complexes (V_Al–O_N, V_Al–2O_N). | Bickermann et al., "The origin of 2.78 eV emission and yellow coloration in bulk AlN substrates," Appl. Phys. Lett. 95, 262104 (2009). |
| Si impurities (growth interface) | Not independently constrained. Current model placeholder (1.0×10⁴ dB/m) has no literature support. | Siₐₗ predicted/observed above ≈10¹⁷ cm⁻³. Its optical signature is entangled with the same broad C/O absorption bands above, not separately resolved in any source found. | (Qualitative context only — no isolated quantitative source found.) |
| Oxidation ingress (sidewall) | No literature value found. Current placeholder (2.5×10⁴ dB/m) is an engineering assumption only. | — | — |
| Sidewall contamination (Si) | No literature value found. Current placeholder (1.5×10⁴ dB/m) is an engineering assumption only. | — | — |
| Sidewall damage | No literature value found. Current placeholder (5.0×10⁴ dB/m) is an engineering assumption only. | Dry-etch damage is well documented qualitatively in GaN/III-N devices (increased roughness, surface non-radiative recombination) but not quantified as an absorption coefficient for AlN specifically. | General III-N dry-etch-damage literature (qualitative only — no citation with a directly usable number found). |

Table 1. Literature-informed alpha0 estimates by mechanism, current model placeholders, and supporting citations.

# Caveats

Bulk crystal vs. thin film: the C/O quantitative anchor (60–80 cm⁻¹) comes from 500 µm PVT-grown bulk AlN substrates at [C] ≈ 10²⁰ cm⁻³ — grown specifically for deep-UV LED/laser substrates, not photonic-grade thin films. MOCVD/sputtered/MBE thin-film AlN cores typically carry orders of magnitude lower impurity concentrations. If point-defect absorption scales roughly linearly with impurity concentration (a common first approximation, not independently verified here for AlN), the device-relevant alpha0 could be 2–3 orders of magnitude below the bulk-crystal value — i.e. this table’s C/O numbers are best read as an upper bound, not a working estimate, unless your actual core material’s impurity concentration (e.g. from SIMS) is comparable to the bulk-crystal value.

C and O are not cleanly separable: the cited samples contain both carbon and oxygen/silicon donors simultaneously, and the measured 60–80 cm⁻¹ is the total broadband absorption, not a per-species decomposition. Treating this as an anchor for BOTH the C and O rows (rather than splitting it) is a simplification.

Dislocations are modeled as absorption here, but the literature treats them as a scattering mechanism (a volume-current-method calculation, the same family of method EMode itself uses for sidewall scattering) — localized index/strain perturbations radiate power into non-guided modes, rather than dissipating it as heat. Keeping "Dislocations" in the absorption-mechanism list is a reasonable practical simplification, but a more faithful implementation would add a dislocation-scattering term to scattering_model.py alongside the sidewall Payne-Lacey term, using the literature’s TM > TE finding to also cross-check that scattering_model.py’s all-orientation, total-field-intensity simplification isn’t hiding the same effect.

Si impurities and all three sidewall mechanisms (oxidation ingress, sidewall contamination, sidewall damage) have no supporting literature value at all — their alpha0/L values remain pure engineering placeholders. Sidewall damage/contamination are process-specific enough (dependent on your exact etch recipe and any post-etch treatment) that a literature value from a different group’s process would be of questionable relevance even if one existed; a dedicated XPS/SIMS depth-profile of your own fabricated sidewalls would be the more direct path to a real number.

# References

H. C. Robinson, D. Danilin, M. S. I. Mollik, D. Wickramaratne, J. L. Lyons, V. Fedorov, S. Mirov, and M. E. Zvanut, "Charge-state control of carbon-related optical absorption in AlN," arXiv:2606.19615 (2026).

M. Bickermann, B. M. Epelbaum, O. Filip, P. Heimann, S. Nagata, and A. Winnacker, "The origin of 2.78 eV emission and yellow coloration in bulk AlN substrates," Appl. Phys. Lett. 95, 262104 (2009).

H. Chen, Y. Xie, and Y. Zhao (Arizona State University), "Study of crystalline defect induced optical scattering loss inside photonic waveguides in UV–visible spectral wavelengths using volume current method," Opt. Express 27(12), 17262–17271 (2019).