Loss vs. Dimensions Pipeline

Model description and operating guide

Revision 2 -- adds top/bottom (horizontal) scattering, dual calibration, and the TM00 mode-identity verification tool

# 1. Overview

This pipeline estimates propagation loss (dB/cm) for the fundamental TM00 mode of an AlN ridge waveguide as a function of core height and width, combining two mechanisms: sidewall AND top/bottom scattering (from surface roughness) and non-uniform material absorption (from growth-interface impurities/dislocations and sidewall damage/contamination).

Two complementary computational strategies are used together. EMode (a commercial finite-difference mode solver) provides an initial, physically grounded reference for both mechanisms from a geometry sweep. A set of pure-Python models then reproduce/adapt that physics using the mode-field data exported from that sweep, so that once the initial EMode sweep and a one-time calibration are done, every subsequent exploration of different physical assumptions (roughness magnitude, absorption strength, defect penetration depth, etc.) happens instantly in Python — no further EMode calls, and no further consumption of EMode’s single-seat license.

# 2. Architecture

All files live in loss_vs_dimensions/ (a standalone deliverable, separate from the phase-matching pipeline, though it imports emode_helpers.py from there):

sweep_loss_vs_dimensions.py  —  Drives EMode: for each (h, w) point, builds the waveguide geometry, solves the lossless fundamental mode, computes EMode’s native scattering loss (vertical/horizontal/combined), and exports the mode’s field data for later Python-only reuse. Checkpointed/resumable, with a self-healing CSV schema migration and a live TE_fraction sanity print (see Section 7).

emode_export.py  —  EMode-facing extraction helpers (field/scattering data in the exact shapes EMode’s API returns, confirmed against a live diagnostic run) and the analytic core-geometry mask builder.

inspect_emode_outputs.py  —  One-time diagnostic confirming EMode’s return shapes/units. Already run and confirmed; kept for re-verification if EMode or solver settings change.

absorption_model.py  —  Pure-Python, EMode-free non-uniform absorption model — computes each named physical mechanism’s modal loss contribution from the exported mode profile.

scattering_model.py  —  Pure-Python, EMode-free adaptation of Payne-Lacey scattering theory, computed from the exported mode profile — sidewall (vertical) AND top/bottom (horizontal) terms, each independently calibrated. Needs fitted calibration_factor(s) for correct absolute values.

calibrate_scattering.py  —  Fits scattering_model.py’s vertical and horizontal calibration_factors independently, by least-squares against EMode’s native scattering_vertical_dB_per_m / scattering_horizontal_dB_per_m across a completed sweep; persists both fits.

plot_loss_vs_dimensions.py  —  Plotting/aggregation layer: loads sweep results, bundles every loss-contributor assumption into one dict, and produces the width/height (3-panel: scattering / absorption / total, linear or log-log), mechanism-breakdown, and 3-D surface plots.

verify_mode_profiles.py  —  Post-hoc TM00 mode-identity check, no EMode calls — plots |Ex|/|Ey|/|Ez| for every exported point to field_profile_plots/ and reports a quasi-TE/quasi-TM energy-fraction proxy, so every point (including ones solved before the live check existed) can be visually/numerically verified.

Loss_vs_Dimensions_Dev.ipynb  —  The interactive notebook that drives all of the above, organized into 9 numbered sections (Section 6 of this guide).

# 3. Physics models

## 3.1 Native EMode scattering (Volume Current Method)

For each geometry point, an RMS roughness and correlation length are assigned to the core shape’s sidewalls (vertical interfaces) and top/bottom surfaces (horizontal interfaces) — per EMode’s own convention, both parameters are 2-element lists ordered [vertical, horizontal]. After solving the lossless mode, EMode’s built-in scattering calculation (Volume Current Method) gives the resulting loss separately for vertical and horizontal edges — confirmed empirically that their sum exactly equals the combined value EMode also reports. The pipeline logs all three (vertical / horizontal / combined) separately.

## 3.2 Payne-Lacey-adapted scattering model

scattering_model.py is a from-scratch reimplementation — not a reuse of EMode’s internal calculation — so that once a point’s mode field has been exported, scattering estimates can be recomputed instantly for any assumed roughness/correlation length without touching EMode again. It follows the physical framework of Payne & Lacey’s classic perturbation theory (radiated power proportional to the roughness variance, the guided mode’s field intensity at the boundary, and the roughness’s power spectral density evaluated at the phase-matching condition with the cladding’s radiation continuum), but evaluates the boundary field intensity and guided power directly from the real, simulated 2-D mode profile rather than from the original paper’s idealized 1-D slab-waveguide formulas.

Two independent terms are computed and summed for the "total scatter" reported elsewhere in this pipeline:

Sidewall (vertical): evaluates |E|^2 at the left/right core boundary in every grid row, against a single cladding index (the core is surrounded by the same top-cladding material on both sides in this geometry).

Top/bottom (horizontal): evaluates |E|^2 at the top and bottom core boundary in every grid column, SEPARATELY for the top surface (interfacing the top-cladding material) and the bottom surface (interfacing the substrate) — generally different materials with different index contrast against the core.

Because of this adaptation, the model’s overall absolute scale is not pinned down by first principles and must be fixed empirically, independently for each term (Section 4). Once calibrated, cross-validation across a 105-point sweep (7 heights, 15 widths) showed R² = 0.99 for the sidewall term against EMode’s own native vertical-scattering value, and R² = 0.98 for the horizontal term against EMode’s native horizontal value — aggregate fit quality is good for both, but see Section 7 for an important caveat on the horizontal term’s PER-POINT behavior at extreme aspect ratios.

## 3.3 Non-uniform absorption model

Growth-interface impurities/dislocations and etched-sidewall defects are not uniformly distributed through the waveguide cross-section — they concentrate near the relevant physical boundary and fall off into the bulk. absorption_model.py represents each mechanism as a LOCAL power-absorption coefficient (alpha0, in dB/m) exactly at that boundary, decaying into the core with a chosen functional form (exponential or a hard step) over a characteristic penetration depth (L, in nm). Two localizations are supported: "interface" mechanisms decay upward from ONLY the bottom core/substrate interface (the top surface gets none of this contribution); "sidewall" mechanisms decay inward from BOTH the left and right sidewalls symmetrically.

The resulting modal loss is the Poynting-flux-weighted spatial average of that local profile over the whole mode cross-section. Seven mechanisms are currently modeled — four growth-interface (dislocations, carbon/silicon/oxygen impurities) and three sidewall (oxidation ingress, contamination, mechanical/etch damage) — each independent and additive. See the companion literature-review document for which alpha0/L values are currently grounded in published measurements and which remain engineering placeholders.

# 4. Calibration workflow

Run the EMode sweep (sweep_loss_vs_dimensions.py, Notebook Section 3) across the desired (h, w) grid, with a single, fixed roughness/correlation-length assumption for the whole sweep.

Fit BOTH Payne-Lacey calibration factors (calibrate_scattering.py, Notebook Section 4) by least-squares — the sidewall (vertical) factor against every point’s scattering_vertical_dB_per_m, and the top/bottom (horizontal) factor independently against scattering_horizontal_dB_per_m, each using that point’s own logged roughness/correlation-length values. Reports a per-point comparison table and an R² for each, and persists both fits (plus n_core/n_clad/n_substrate) to scattering_calibration.json.

From this point on, scattering contributions are computed by scattering_model.py using the persisted calibration factors — no further EMode calls are required, even to explore roughness/correlation-length assumptions different from the ones actually used in the EMode sweep, since calibration transfers the overall scale, not a specific roughness value.

# 5. Data flow and outputs

loss_vs_dimensions_results.csv  —  One row per successfully solved (h, w) point: n_eff; EMode’s native scattering loss (combined / vertical-only / horizontal-only, dB/m); the roughness_rms/correlation_length values used; and the path to that point’s exported field data. Self-healing: a schema change (e.g. a new logged column) automatically migrates the file rather than silently corrupting it.

field_exports/h{height}_w{width}.npz  —  Per-point exported mode data: grid coordinates, Ex/Ey/Ez/Sz field components, the analytic core-region mask, n_eff, and the pump wavelength. This is the only file the Python-only models (absorption_model.py, scattering_model.py) actually depend on.

field_profile_plots/h{height}_w{width}.png  —  Per-point |Ex|/|Ey|/|Ez| field-distribution plots from verify_mode_profiles.py, for visually confirming TM00 mode identity (see Section 8 for an example).

scattering_calibration.json  —  The persisted calibration_factor (vertical) and calibration_factor_horizontal, their respective r_squared values, n_core, n_clad, n_substrate, and how many points the fit used.

Example (current, from a 105-point sweep): calibration_factor=0.922 (R²=0.990), calibration_factor_horizontal=1.302 (R²=0.983), n_core=2.111, n_clad=1.47, n_substrate=1.776. These numbers change every time the sweep or calibration is re-run — treat this as an illustration of the schema, not a fixed reference value.

# 6. Operating the notebook

Loss_vs_Dimensions_Dev.ipynb is organized into 9 sections. The first four involve EMode (license/time cost); the rest are pure Python and effectively instant.

| # | Section | What it does | Cost |
| --- | --- | --- | --- |
| 1 | Verify the core geometry mask convention | One-time visual sanity check. | EMode |
| 2 | Re-run the EMode-output diagnostic (optional) | Only needed again if EMode’s return-value shapes are suspected to have changed. | EMode |
| 3 | Run the loss-vs-dimensions sweep | The main step. Sweep range (heights/widths) is editable directly in the notebook cell; checkpointed, so interrupting or extending the range only costs the new points. | EMode |
| 4 | Fit scattering-model calibration factors | Reads the sweep’s results, no EMode call. Fits vertical AND horizontal factors. Re-run any time the sweep gains new points. | Python |
| 5 | Plot results | Top-level totals plot, using the calibrated Python model rather than the raw EMode number. | Python |
| 6 | Explore absorption assumptions interactively | Earlier single-mechanism scratch cell; superseded in practice by Section 8. | Python |
| 7 | Compare Payne-Lacey (adapted) vs. EMode-native scattering | Calibration cross-check plot (sidewall-only, both models, same roughness assumption). | Python |
| 8 | Live loss-contributor assumptions | The primary day-to-day workflow. Fully self-contained. One cell holds every tunable input (sidewall AND top/bottom sigma/Lc, n_core/n_clad/n_substrate, both calibration factors, all mechanisms) in one place — edit and re-run to update the 3-panel width/height plot, per-mechanism breakdown, and 3-D loss-vs-(h,w) surface immediately. | Python |
| 9 | Verify TM00 mode identity across the sweep | Plots ¦Ex¦/¦Ey¦/¦Ez¦ and a quasi-TE/quasi-TM energy-fraction proxy for every exported point, to field_profile_plots/ — works even on points solved before this check existed. | Python |

Table 1. Notebook sections, what each does, and whether it consumes the EMode license.

Day-to-day workflow once a sweep and calibration exist: reload the notebook file, jump straight to Section 8, edit the assumptions cell, re-run the plotting cell. Sections 1–4 only need to be re-run when adding new (h, w) geometry, changing roughness assumptions, or after a schema/code change. Section 9 is a good habit to re-run after any new sweep, to catch a mode-identity problem before trusting the numbers.

# 7. Example: TM00 mode-profile verification

Output of verify_mode_profiles.py for one point (h=340 nm, w=400 nm) from the current sweep. |Ey| (center) shows a clean, single-lobe fundamental-mode profile centered in the core (orange outline) — the hallmark of a well-identified TM00 mode. |Ex| (left) shows the characteristic four-lobe cross-polarization pattern expected for the weak orthogonal component at a rectangular index discontinuity (real physics, not a defect). |Ez| (right) shows the expected two-lobe longitudinal component. This point’s energy-fraction proxy was Ex=0.1%, Ey=93.3%, Ez=6.5% — far below the 10% flag threshold.

Figure 1. Example TM00 mode-profile verification plot (h=340 nm, w=400 nm).

# 8. Known limitations and open items

The horizontal (top/bottom) Payne-Lacey scattering term’s aggregate fit quality looks good (R²=0.98 across 105 points), but its PER-POINT residuals diverge badly for tall, narrow cores: ratios of calibrated-model to EMode-native reach ~2–3× for h ≥ 600 nm at w ≤ 400 nm, while the sidewall (vertical) term stays within ~±20% across the whole grid. Treat "total scatter" and "total loss" results with more caution than sidewall-only ones for that geometry range until this is investigated further — the likely cause is the top/bottom boundary-intensity simplification breaking down at extreme aspect ratios, but this hasn’t been confirmed.

The core-boundary geometry mask (used by both Python-only models to know where the waveguide cross-section actually is) is reconstructed analytically from the nominal (h, w, sidewall_angle) parameters rather than read back from EMode’s own solved permittivity map. It has been cross-checked visually against EMode’s own shape/index plot for one representative geometry, not validated across the full sweep range.

scattering_model.py’s absolute scale depends entirely on the empirical calibration factors; if the assumed core/cladding/substrate refractive indices, roughness statistics, or wavelength change substantially from what was used to derive the current fits, they should be re-validated.

The TM00 mode-identity check (Section 9 / verify_mode_profiles.py) uses an E-field energy-fraction proxy, not EMode’s own internal TE_fraction calculation (which may use the H-field structure, not exported here). It correlates well and found zero flagged points across the current 105-point sweep, but is not guaranteed to exactly match EMode’s number in every case — the field plots themselves remain the more trustworthy check.

Several absorption mechanisms (silicon impurities; all three sidewall-specific mechanisms) currently have no supporting literature value for their alpha0/L parameters — see the companion literature-review document.

Dislocations are modeled here as an absorption mechanism for practical simplicity; the literature actually treats dislocation-induced loss as a scattering process, with a documented TM > TE polarization dependence not currently reflected in either the absorption or scattering model.